## Slide 1: PLAIN CONCRETE
WORKABILITY

## Slide 2: WORKABILITY
Workability of Fresh Concrete is a property related with its ease of transportation, placing, compaction and finishing without any detrimental effects such as segregation and bleeding
Segregation of concrete means separation of concrete constituents accompanied by settling of bigger particles
A coherent and almost homogenous mass of concrete is actually required

## Slide 3: WORKABILITY
Bleeding of concrete means separation of cement slurry from the concrete mass
Usually , either this paste comes on top of concrete surface or leaks through pores in the formwork
Workability requirements for a mass concrete work are significantly different from that of concreting in thin or heavily reinforced sections

## Slide 4: WORKABILITY
Workability of fresh concrete is to be judged based on three aspects; Compactibility, Mobility, and Stability
Compactibility refers to the ease with which concrete is compacted and air voids are removed
Mobility is a measure of the ability of concrete to flow into the molds and around the reinforcement
Stability is a property of fresh concrete to remain as a coherent homogenous mass during handling and vibration without segregation and bleeding

## Slide 5: WORKABILITY
When ingredients of concrete are mixed in dry state air voids are entrapped within the particles
After addition of water and wet mixing, air bubbles may automatically move up due to their lesser density
The only obstruction to this movement of the air bubbles is caused by the surrounding thick paste and the aggregate particles due to mechanical interlocking and chemical adhesion

## Slide 6: WORKABILITY
If concrete particles move relative to each other the air bubbles may find their way up and may escape
To reduce friction between particles water or plasticizers may be added
Friction between the particles can be reduced by rodding or vibration of concrete
Quantitatively, a good measure of workability is the useful internal work or energy required to overcome the internal friction between particles

## Slide 7: HONEYCOMBING
Strength of hardened concrete is significantly reduced if voids are left in the compacted concrete mass
Honeycombing is used to describe the presence of large and usually interconnected voids in the concrete showing extremely poor quality concrete produced by escape of fine particles along with slurry of cement and water

## Slide 8: Average Strength Reduction Due to Voids
The average reduction in concrete strength by the presence of voids
Voids Percentage | Strength Reduced
2% | 10%
5% | 30%
10% | 55%
20% | 85%

## Slide 9: Average Strength Reduction Due to Voids
Water required for hydration of cement is approximately 25% of the weight of cement
However, concrete made by using this W/C ratio, it will be very dry and almost impossible to compact
A considerably large amount of work is required to liberate the air between the particles
Voids in hardened concrete may be either bubbles of entrapped air or spaces left by evaporation of excess water

## Slide 10: Average Strength Reduction Due to Voids
Lesser amount of water in the mix may leave bubbles of entrapped air and
Using more water may lead to more spaces left by excess water
The best amount of water to be added is that which keeps the sum of volumes of both types of voids to a minimum

## Slide 11: Factors Affecting Workability Available for a Mix
Water content
Aggregate type
Aggregate grading
Aggregate/Cement ratio
Presence of admixtures
Fineness of cement
Time required for mixing, transportation, placing and compaction of concrete
Prevailing temperature and humidity
Air entrainment

## Slide 12: Factors Affecting Workability Available for a Mix
A well designed mix with such a water content that gives a coherent mass but allows easy placing and compaction for the given means of compaction, type of construction and type of formwork is usually desirable
Porosity, surface texture, size and shape of particles influence the workability of a concrete mix
A well graded aggregate with spaces between the larger filled by the smaller particles avoids segregation

## Slide 13: Factors Affecting Workability Available for a Mix
When aggregate over cement ratio is low more particles will be finer resulting in a higher total surface area of solids
Plasticizers and super plasticizers are used in concrete to improve the workability up to a large extent at a given water cement ratio without adversely affecting the strength
Extreme case possible with the help of super plasticizer is to get flowing and self compacting concrete with lesser W/C ratio and no segregation

## Slide 14: Factors Affecting Workability Available for a Mix
Accelerators may reduce workability depending on the time consumed after mixing of water in the concrete
Finer cement require more water for a workable mix
After initial mixing, workability reduces after evaporation of water, absorption by aggregate and stiffening of cement gel

## Slide 15: Factors Affecting Workability Available for a Mix
A higher temperature and low humidity condition reduces the workability due to more loss of water and quicker stiffening of cement gel
Above 50o C with relative humidity lower than 20%, workability reduces
Entrapped fine bubbles of air intentionally added improves workability and resistance against frost action but is associated with some loss of strength

## Slide 16: Tests for workability
Slump test
Compacting factor test
Vebe test
Flow table test
Ball penetration test

## Slide 17: Admixtures and Additives
Any chemical/substance added to cement during its manufacture to improve the quality of concrete or to obtain any desired effect on concrete is called additive.
Any substance added to concrete during its mixing to improve its quality in a desired way is called admixture

## Slide 18: Admixtures
Admixtures may be of general types
Accelerators
Set Retarders
Plasticizers or water reducers
Super Plasticizers
Cement admixtures
Gas forming or air entraining agents
Bonding admixtures
Sealing agents

## Slide 19: Admixtures
Accelerators
  Accelerate the hardening of concrete in order to get development of early strength
  Quick setting admixtures are also available which case flash set such as washing soda or sodium carbonate
Set retarders
  Cause delay in setting of concrete and are useful for mass concreting,
  concreting in hot weather, improving construction joints, obtaining special architectural finishes

## Slide 20: Admixtures
Plasticizers or water reducers
  Reduce amount water required for desired workability
  Reduction in water cement ratio increases strength of concrete
  Hence maintaining same strength and workability, cement content may be reduced for economy and for controlling heat of hydration in mass concrete

## Slide 21: Admixtures
Super plasticizers
  Preferably suphonated naphthalene formaldehyde condensates and
  Sulphonated melamine formaldehyde condensates
  Helpful in maintaining very low water cement ratios and to achieve very high strength
  May increase slump from 75mm to 300mm for the same strength and cement content

## Slide 22: Admixtures
Cementing admixtures
  Use of pozzolans, blast furnace slag and lime in concrete provides cementitious properties
  Pozzolans provide cementitious properties and may replace cement up to 40%
  Greater advantage is slow rate of hydration and heat development
  Volcanic ash, pumicite, opaline shales, calcined diatomaceous earth, burnt clay, fly ash and pulverized fuel ash may act as pozzolans

## Slide 23: Admixtures
Gas forming or air entraining admixtures
  Used to liberate gas in fresh concrete so as to form aerated or foam concrete, which is light weight and provides better thermal insulation
  Introduce very fine air bubbles to improve their resistance against frost action
Bonding admixtures
  Improves bond between fresh and already hardened concrete
Sealing agents
  Reduce capillary absorption of water by concrete

## Slide 24: Compressive strength of concrete
Concrete strength is indeed controlled by limiting strain rather than a maximum stress level
In pure tension, concrete fails at a strain value within the range 0.0001 to 0.0002
The compressive strain causing failure is approximately 0.002 for a 70MPa concrete to 0.004 for a 14MPa concrete

## Slide 25: Mechanism of Concrete Failure in Compression
Very fine cracks are present in hardened concrete at the surface of coarse aggregate before the application of load are called bond cracks
The bond cracks do not open up to 30% of Ultimate strength
At stress level approximately 30 to 70% of ultimate strength, cracks grow in number, length and width
At this stage, stress strain curve become nonlinear

## Slide 26: Mechanism of Concrete Failure in Compression
In this range of stress, cracks are not usually interconnected with each other and are termed micro-cracks
At stress level 70 to 90%, cracks through mortar appear that connect the bond cracks to form large interconnected cracks

## Slide 27: Factors Affecting Strength of Concrete
Porosity
  Main factor that influences strength
  Pores are produced in hardened concrete due to two main reasons
    Presence of entrapped air in the concrete
    Evaporation of water from the hardened concrete
  Water added to concrete mix remains as gel water and capillary water in the hardened moist cured concrete
  Combined water is the water that is chemically combined or permanently held within crystals as water of hydration

## Slide 28: Factors Affecting Strength of Concrete
Combined water does not evaporate upon drying up to 105oC and amounts to approximately 23% of mass of dry cement
Gel pores are very small pores of about 2 x 10-6mm diameter
Gel water is approximately 28% of cement gel volume
Capillary pores are relatively larger pores 0.001mm in diameter formed within gel
The volume of these pores is approximately 18.5% of dry volume of cement provided

## Slide 29: Factors Affecting Strength of Concrete
Capillary pores may be filled with capillary water during moist curing.
At a W/C of 0.6, all types of pores for fully compacted concrete may occupy 47 to 60% volume of cement paste.
Strength of concrete not only depends upon total volume of pores but also upon the other features such as whether these pores are interconnected or they are separate.

## Slide 30: Factors Affecting Strength of Concrete
Degree of compaction
  It is related with removal of air voids from the concrete
  If full compaction is not carried out air voids are left in concrete
Water cement ratio
  Larger W/C from the basic value required for full hydration reduces the strength drastically by increasing the porosity of cement gel

## Slide 31: Factors Affecting Strength of Concrete
Age of concrete
  Strength of concrete increases with age
  This is caused by hydration of cement and reduction of capillary pores
  This effect is more pronounced at early ages and becomes slow at higher ages
  At an age of one year the effect is insignificant
Improper curing and temperature changes
  It produce shrinkage and thermal cracks

## Slide 32: Factors Affecting Strength of Concrete
Aggregate/Cement ratio
  For a constant W/C and full compaction, a leaner mix with larger aggregate/cement ratio develops higher strength
  This effect is produced due to lesser porosity of the resulting concrete
Aggregate properties
  Grading, surface texture, shape, strength and maximum size of aggregate also influence the concrete strength

## Slide 33: Factors Affecting Strength of Concrete
  Bond cracks may easily develop and propagate for smooth gravel than for rough and angular crushed aggregate
  Crushed aggregate may develop larger strengths
  For high strength concretes, failure planes may pass through the larger size aggregate particles and their individual strength also becomes significantly important

## Slide 34: Factors Affecting Strength of Concrete
Effect of additives and admixtures
  It may influence the strength of concrete.
  Strength at ages lesser than 28 days are effected the most.
  Final strengths may also vary with type of cement and presence of any additional chemical in it.